### SECTION 611 – CONCRETE SLOPE PAVING

**MATERIALS**

**611.02.01 GENERAL**

***DELETE PARAGRAPH “C” AND REPLACE WITH THE FOLLOWING:***

C. Reinforcing for the slope paving and cutoff walls shall be reinforcing steel in accordance with the Contract Drawings and Section 505.

***add The following to this subsection:***

F. Concrete for the concrete slope paving and cutoff walls shall be modified Class A or AA using Type V cement (6.0 sack minimum, 0.53 water/cement ratio), having a minimum twenty-eight (28) day compressive strength of 3000 psi having a slump not to exceed 4-inches.

**METHOD OF MEASUREMENT**

**611.04.01 MEASUREMENT**

***add The following to this subsection:***

The quantity of CONCRETE SLOPE PAVEMENT will be measured per square yard.

The quantity of [FILL IN ITEM DESCRIPTION] will be measured per [UNIT].

No direct measurement shall be made for [FILL IN ITEM DESCRIPTION].

**BASIS OF PAYMENT**

**611.05.01 PAYMENT**

***add The following to this subsection:***

The accepted quantity of CONCRETE SLOPE PAVEMENT will be paid for at the contract unit price of square yard and shall conform to the requirements of subsection 611.05.01 of the Uniform Standard Specifications and shall include all materials, equipment, labor and disposal required to perform this work and all work as shown on the Plans, as specified herein and as directed by the Engineer. The above payment shall also include,

The accepted quantity of [FILL IN ITEM DESCRIPTION] will be paid for at the contract unit price of [UNIT] and shall include all materials, equipment and labor required including, but not limited to, [FILL IN] and all other items necessary to complete the work as shown on the Plans, as specified herein and as directed by the Engineer.

Unless otherwise provided in the Special Provisions, no payment will be made for [FILL IN ITEM DESCRIPTION] as such. The cost thereof shall be considered as included in the price bid for construction or installation of the items to which [FILL IN ITEM DESCRIPTION] is required.

Payment will be made under:

|  |  |  |
| --- | --- | --- |
| **ITEM NO.** | **ITEM DESCRIPTION** | **UOM** |
| 611.0010 | CONCRETE SLOPE PAVEMENT | SY |

**END OF SECTION 611**